## Biobased Roof Edge Profile for Green Roofs

Supplier:
New Circle B.V.

## Product description

Biobased roof edge profile intended for the edge finishing of extensive sedum roofs and green roofs. The profile prevents the washing away of substrate and serves as a separation between vegetation, substrate and vegetation-free zones.

## System description

The biobased roof edge system by New Circle consists of a biobased roof edge profile and the corresponding biobased connectors. All system components are manufactured from biobased HDPE and designed as an integrated circular system.

By using exclusively biobased components, a consistent and durable roof edge finish for green roofs is achieved without compromising technical performance, service life or ease of installation.

The system is suitable for extensive sedum roofs and green roofs and functions as a separation between vegetation, substrate and vegetation-free zones.

## Material

Biobased HDPE, manufactured from renewable raw materials.
Biobased content: minimum 98%.

## Dimensions

Length: 2000 mm
Width: 60 / 80 mm
Height: 60 / 80 mm
Thickness: 2.7 mm

## Colour

Graphite (RAL 7024)

## Weight

Approx. 1.2 kg per unit

## Technical properties

- Dimensionally stable and impact resistant

- UV-resistant

- Resistant to weather conditions and temperature fluctuations

- Fully recyclable

- Technical service life: approx. 50 years

## Sustainability

CO₂ emission: –1.97 kg CO₂-eq per kg of material.

The product therefore provides a demonstrably positive environmental impact.

## Installation

Roof edge profiles are connected to create a continuous edge finish. The profile can optionally be bonded with a suitable fixing adhesive. In certain applications bonding is not strictly necessary and the product is held in place by the green roof build-up.

## Guidelines

Installation in accordance with applicable green roof guidelines and supplier instructions.